Supplementary Data

Free-standing nanocomposites with high conductivity and extensibility

Kyoung-Yong Chun1, Shi Hyeong Kim1, Min Kyoon Shin1, Youn Tae Kim2, Geoffrey M. Spinks2, Ali E. Aliev3, Ray H. Baughman3 and Seon Jeong Kim1*

1 Center for Bio-Artificial Muscle and Department of Biomedical Engineering, Hanyang University, Seoul, 133-791, Korea

2 IT Fusion Technology Research Center and Department of IT Fusion Technology, Chosun University, Gwangju, 501-759, Korea
3 ARC Centre of Excellence for Electromaterials Science, Intelligent Polymer Research Institute, University of Wollongong, Wollongong, NSW, 2522, Australia

4 The Alan G. MacDiarmid NanoTech Institute, University of Texas at Dallas, Richardson, TX 75083, USA

*E-mail: sjk@hanyang.ac.kr

Figure S1. Apparatus used for electrical conductivity measurements as a function of applied tensile strain.

Figure S2. Schematic diagram of measurement setup for 3 method.

Thermal conductivity and electrical resistivity measurements:

The thermal conductivity and thermal diffusivity of CNT composite were measured using the self heating 3-omega method. At low frequencies the 1D heat flow can be expressed in the terms of the third-harmonic voltage signal U3  induced by an AC current Io∙sint applied through the elongated sample (metallic wire, carbon fiber, nanotube or bundle, yarns or sheet). The AC current with frequency  creates a temperature fluctuation in the specimen at double the driving frequency, 2.  The interaction of the 2 modulated resistance R with the 1 current will create a third harmonic response on the potential electrodes [S1],

,  				(1)

where I=UI /R is the applied constant–amplitude AC current, R is the specimen resistance between the current electrodes, R=(dR/dT) is the temperature gradient of the resistance at room temperature, L is the distance between potential electrodes, S is the cross-sectional area of the sample, κ is the thermal conductivity, =L2/2∙α is the characteristic thermal time constant of the specimen for the axial thermal process, and α = κ/∙Cp as defined above is the thermal diffusivity. The diffusivity can be obtained from the frequency dependence of the phase lag of the third-harmonic signal,

,					(2)

or from the frequency dependence of the 3ω  signal, U3ω, from the Eq. (1). For thin and long specimens in the low frequency limit one obtains the thermal conductivity,

.					      (3)

Figure S3. The chemical structure of the polystyrene-polyisoprene-polystyrene (SIS) polymer (top) and the stress-strain curve (bottom) of this SIS polymer, MWNT-SIS, and Ag-MWNT-SIS composites where the strain is engineering strain.

a

b

Figure S4. Data on the structure and composition of AMSN films in which Ag nanoparticles are mixed with MWNTs in a SIS matrix. The area bordered by the pink line in the SEM micrograph of (Fig. S2a) was characterized by energy dispersive X-ray analysis (EDS) (Fig. S2b). The concentration of Ag nanoparticles in this composite film was 29 vol% in the dried film corresponding to the 34 wt% of Ag in the initial mixture.

2 wt%

1 wt%

3.5 wt%

0.3 wt%

7 wt%

Figure S5. The morphology of composite (MWNT-SIS) films according to the concentration of MWNTs. The homogeneous MWNT films are prepared with blending with an ionic liquid and the polystyrene-polyisoprene-polystyrene (SIS) copolymer. However, the film is cracked from 3.5 wt%. The diameter of all glass petri-dishes is 5 cm.

Figure S6. Film resistance as a function of the concentration of MWNTs.

The concentration of MWNTs versus a SIS copolymer including ionic liquid is presented. The weight ratio of an ionic liquid versus MWNTs was 2.5 and the weight of SIS was 2.6g in the initial mixture.

Movie S1. Movie picture of the operation of PC fan using AMSN film as an electronic interconnect, where this film is strained up to 30% during fan operation.

Reference

[S1]	Lu L, Yi W and Zhang DL, 3ω method for specific heat and thermal conductivity measurements 2001 Review of Scientific Instruments 72 2996.